## Slide 1: Neutrons and Li-ion batteries: A perfect marriage
Christian Masquelier (LRCS),
Laurence Croguennec (ICMCB),
Emmanuelle Suard (ILL)
Matteo Bianchini
ILL
ICMCB
LRCS
Notes: These sur financement ILL

## Slide 2: Summary:
Neutron Diffraction Experiments In Real Time
Introduction: Li-ion batteries, why neutrons and why operando ?
Conclusion
Spinel materials:
Li1+xMn2-xO4
LiNi0.4Mn1.6O4
A new Electrochemical cell to study Li-ion battery materials
Applications
How ?

## Slide 3: Working principle of Li-ion batteries
Positive Electrode
LiFePO4
Separator/Electrolyte
EC:DMC - LiPF6
Negative Electrode
Graphite
Discharge
Li1+Fe2+ (PO4)3-
Fe3+ (PO4)3-
Reduction
Notes: STRESS on structural evolution

## Slide 4: The Goal: Diffraction in real time…
In situ & Operando
Notes: The first and most challenging point has been to develop…

## Slide 5: The Goal: Diffraction in real time…
In situ & Operando
Electrode materials studied ex situ risk to be exposed to atmospheric agents (even in gloveboxes)
Electrochemical reactions are dynamical processes
Metastable phases are often encountered
High-rate cycling means non-equilibrium conditions
Operando studies reproduce as much as possible
real-battery working conditions
Notes: The first and most challenging point has been to develop…

## Slide 6: The Goal: Diffraction in real time…
good electrochemical performances
REFINABLE neutron diffraction (ND) powder patterns
An electrochemical cell for
In Situ NEUTRON DIFFRACTION
In situ & Operando
…with neutrons
Notes: The first and most challenging point has been to develop…

## Slide 7: Neutrons: Challenges vs. Why do we care?
  Neutrons’ sensitivity to Lithium!
  Neutrons’ contrast between neighbouring elements
  Neutrons probe the whole electrode
MAIN ISSUES | ND | Electrochem. | Solution
amount of powder required | > 120 mg | < 250 mg | 200 mg
hydrogen-rich electrolytes | High backgound | OK | Deuterated Electrolytes (costly)
Neutron scattering lengths
Notes: There are a number of issues related to the use of neutrons
ONLY SAY QUICKLY DEFECTS
-big electrodes to sample
-h scatters neutrons incoherently

## Slide 8: A new electrochemical cell for in situ neutron diffraction
Powder (positive electrode)
TiZr current collector
Li metal (negative electrode)
TiZr container
Mylar foil
Spring
Separator
Gasket
Plunger
M. Bianchini, J.B. Leriche, J.-L. Laborier, , L.Gendrin, E.Suard, L. Croguennec, C.Masquelier, J. Electrochem. Soc., 160(11), A2176, 2013
A new Null Matrix electrochemical cell for Rietveld refinements of in situ or operando neutron powder diffraction data
Notes: CAREFUL: TIZR!!!!! Neutron transparent! And good conductor and resist oxydation and chemical corrosion
IMPORTANCE OF D20 AS WELL

## Slide 9: D20 @ ILL (High Flux) – Experimental Setup
Detector
Neutrons beam
Potentiostat‘s
connections
In situ
Cell
Notes: Position sensitive detector

## Slide 11
LiFePO4 in the in-situ cell,
in a full-battery configuration,
measured on D20
20
40
60
80
100
120
140
2θ (°)
36
39
42
54
57
60
63
LiFePO4 powder
In-situ: LiFePO4+Csp // electrolyte
Pnma
a=10.3233(2) Å
b=6.0044(1) Å
c=4.6918(1) Å
LiFePO4 POWDER
measured on D2B
Galvanostatic cycling
Cell Validation: LiFePO4
D2B λ=1.594Å, T=298K
D20 λ=1.547Å, T=298K

## Slide 12: In-situ ND of a LiFePO4 battery
2θ (°)
C/24
Intensity (a.u.)
Intensity (a.u.)
Voltage vs. Li+/Li
Time (h)
30
40
50
60
70
80
90
4.2
3.9
3.6
0
4
8
12
16
20
24
30
35
40
2θ (°)
LiFePO4
Rietveld
refinement

## Slide 13: Applications: LiMn2O4 positive electrodes
Li1.10Mn1.90O4
A set of 3 samples:
Cubic LiMn2O4
Li1+xMn2-xO4
(or [Li]Td[LixMn2-x]OhO4)
Capacity
fading
Smaller capacity
BUT NO capacity fading
LiMn2O4
Li1.05Mn1.95O4
After Cell Validation using well-known battery materials
M. Bianchini, J. B. Leriche, J.-L. Laborier, L. Gendrin, E. Suard, L. Croguennec and C. Masquelier, J. Electrochem. Soc. (2013), 160 (11), A2176.
M. Bianchini, E. Suard, L. Croguennec and C. Masquelier, Journal of Physical Chemistry C (2014), 118(45), 25947
Notes: Chute rapide du potentiel

## Slide 14: Electrode charge (C/20) in real-time
95 100 105 110 115
0
5
10
15
20
25
30
35
2θ (°), λ=1.547 Å
Scan number = Time(h)*2
95 100 105 110 115
0
5
10
15
20
25
30
Scan number = Time(h)*2
95 100 105 110 115
0
4
8
12
16
20
24
Scan number = Time(h)*2
LiMn2O4
Li1.05Mn1.95O4
Li1.10Mn1.90O4
Charge
Charge
Charge
2θ (°), λ=1.547 Å
2θ (°), λ=1.547 Å
Peak Intensity
Notes: Diagramme 2D
Domain de miscibilité

## Slide 15
Electrode charge (C/20) in real-time

## Slide 16: High-Voltage spinel materials: LiNi0.4Mn1.6O4

## Slide 17: High-Voltage spinel materials: LiNi0.4Mn1.6O4

## Slide 18: High-Voltage spinel materials: LiNi0.4Mn1.6O4

## Slide 19: High-Voltage spinel materials: LiNi0.4Mn1.6O4

## Slide 20: Conclusions (1st part):
ND gives unique insight on lithium’s
crystallographic information and dynamics
  Design of the (Ti,Zr) electrochemical cell
  Commercial electrodes were used for characterization
  First real study (spinels Li1+xMn2-xO4)
  Study of High-Voltage spinels LiNi0.4Mn1.6O4

## Slide 21: Summary and Conclusion
X-Rays / Synchrotron
& Neutrons Diffraction
In Situ / Operando
& Ex Situ
Crystal structure ↔ Electrochemical properties of electrode materials
Better Li-ion and Na-ion batteries…
(…hopefully)

## Slide 22: Acknowledgements
Nicolas Brisset (ICMCB)
Philippe Dagault (ICMCB)
François Fauth (ALBA)
François Weill (ICMCB)
Erik Elkaim (SOLEIL)
Jean Noel Chotard (LRCS)
Mathieu Morcrette (LRCS)
Jean Marcel Ateba-Mba (ICMCB)
Jean Bernard Leriche (LRCS)
Ludovic Gendrin (ILL)
Jean-Luc Laborier (ILL)
Thomas Hansen (ILL)
Fabien Lalere (LRCS)
Thibault Broux (ICMCB)
My supervisors:
Christian Masquelier (LRCS)
Emmanuelle Suard (ILL)
Laurence Croguennec (ICMCB)
ALBA, Barcelona
ILL, Grenoble
SOLEIL, Paris
My collaborators & everyone who helped me:
Helmut Schober (ILL)
Laurent Chapon (ILL)
Henry Fisher (ILL)
Pierre Bordet (CNRS)
Elena Bogdan (ICMCB)
Dany Carlier (ICMCB)
Yue Deng (LRCS)
Juan Rodriguez-Carvajal (ILL)

## Slide 23: Thank you for your attention!
ILL is acknowledged for financial support and beamtime